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	Reinforced bitumen sheets for roof waterproofing EN 13707

	Product description
	

	Use
	Eave strip

	Application
	Mechanical fastening  

	Reinforcement
	Reinforced polyester

	Coating
	SBS modified bitumen

	Surfacing
	Slate and/or mineral granules

	Bottom surfacing
	Release film and adhesive bitumen

	Characteristic
	Method
	Unit
	Nominal value
	minimum
	maximum

	Length
	EN 1848-1
	m
	10
	-
	-

	Width 
	EN 1848-1
	m
	0,250
	0,245
	0,255

	Mass per unit area
	black

mix color

basic color
	EN 1849-1
	g/m²
	4400

4200

4000
	4180

3990

3800
	-

	Nominal thickness
	EN 1849-1
	mm
	3,6
	3,4
	3,8

	Straightness
	EN 1848-1
	mm / m
	pass
	
	20/10

	Visual defects
	EN 1850-1
	-
	no defects

	Declaration of performance  
	007.CPR.RK

	AVCP- class
	2+

	Certificate of factory production control
	0809-CPR-1030

	Fire properties
	Method
	Classification
	Fireclass

	Reaction to fire
	EN ISO 11925-2
	EN 13501-1
	NPD

	External fire performance
	ENV 11871)
	EN 13501-5
	BROOF(t2)

	Characteristic
	Method
	Unit
	Nominal value
	minimum
	maximum

	Watertightness
	EN 1928 B 
	kPa
	pass
	300
	

	Tensile strength 

- in longitudinal direction 

- in transverse direction
	EN 12311-1

 
	N/ 50 mm

N/ 50 mm
	750

550
	600

400
	900

700

	Elongation

- in longitudinal direction 

- in transverse direction
	EN 12311-1

 
	%

%
	40

40
	25

25
	55

55

	Nail shank tear resistance

- in longitudinal direction 

- in transverse direction
	EN 12310-1


	N

N
	250

300
	150

150
	350

450

	Resistance to static loading
	EN 12370 A
	kg
	NPD
	
	

	Resistance to impact
	EN 12691
	 mm
	NPD
	
	

	Pliability 

- surface

- bottom
	EN 1109
	°C

°C
	-20

-20
	-20

-10
	

	Pliability after ageing

- surface

- bottom
	EN 1296/1109
	°C

°C
	-15

-10
	-10

0
	

	Adhesion of granules
	EN 12039
	%
	 8
	0
	30

	Flow resistance at elevated temperature  
	EN 1110
	°C
	80
	80
	

	Flow resistance at elevated temperature after ageing
	EN 12961110
	°C
	80
	80
	

	Dimensional Stability
	EN 1107-2
	%
	0,3
	
	0,6

	Dangerous substances2),3)
	
	
	No dangerous substances

	1) see: www.kerabit.fi/tuotteet
2) No asbestos or coal tar constituents 

3) In the absence of European harmonized test methods, verification and declaration on release/content has to be done taking into account national provisions in the place of use
	NPD = no performance determined
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This publication has been reviewed with the utmost care. However, we are not liable for any direct or indirect damage resulting from errors or the incorrect application of the information contained herein. We reserve the right to make changes. The latest version of this document is available at kerabit.fi/tuotteet.
